## Slide 1: PPG Spectracron® VRPTM Primer
Robust Corrosion Resistance

## Slide 2: Spectracron® VRPPE
Solventborne Primer
Availability | Technology | Coating Type | Chemistry | Substrates
USCA – MTO | Liquid Solventborne | Primer | 2K Epoxy | CRS, HRS, Galvanneal Steel, Galvanized Steel, Aluminum, Shot Blast Steel and Cast Iron
PPG Segments
Agriculture and Construction Equipment
Transportation
General Industrial
Suggested Uses
Agriculture Equipment
Construction Equipment
Material Handling
Recreational Vehicles
Truck Bodies and Beds
Electrical
Features | Potential Customer Benefits
Strong corrosion performance | Protects assets and increases product longevity
Multi-metal compatibility | Reduces process complexity, footprint and costs
Excellent pop and sag performance | Lowers application cost and rework
Wide application and recoat window | Provides flexibility in process conditions
Wet-on-wet capable | Increases throughput and decreases process cost
Customizable colors | Allows differentiation through color
2.8 lbs./gal. VOCs, less exempts and specifically formulated without HAPs | Reduces cost related to environmental controls
Initially introduced into the OEM agriculture and construction equipment segment this primer technology has demonstrated value to our customers.
Notes: Strong corrosion performance – meets highest level of OEM specifications – JDM F17X1: Level 3, CAT 1E2960 and CNH MAT0103, Class 3P

## Slide 3: Spectracron® VRPPE
Solventborne Primer
Product Characteristics* |  | 
Color | - | Gray & Buff, tintable
Gloss at 60º | ASTM D523 | > 60
VOCs | - | 2.8 lbs./gal. (336 g/L), less exempts
Cure | - | Oven Time/Temp: 20-60 min @ 120-200°F Wet on Wet: 5 min flash, topcoat bake
Performance Properties* |  | 
Pencil Hardness | ASTM D3363 | 4H
Conical Mandrel Bend | ASTM D522 | 1/8”
Impact Resistance, Direct / Reverse | ASTM D2794 | 80 / 20 in-lbs
Chemical Resistance (diesel, water, oil immersion) | ASTM D1308 | 500 hours
Humidity Resistance | ASTM D2247 | 1,000 hours
Salt Spray Resistance | ASTM B117 | >1,000 hours
Cyclic Corrosion Resistance | SAE J2334 | >40 cycles
Compatible Products
Topcoats: Spectracron SPU77777, Spectracron SPU79367, Spectracron SPU65250B, Spectracron HSX, Spectracron HSL, Spectracron VRPT
*results obtained over iron phosphate pretreated CRS panels. Salt spray performance dependent on pretreatment used.
Key Features
Strong corrosion performance
Multi-metal compatibility
Excellent pop and sag performance
Wide application and recoat window
*For specific product VOC information refer to the environmental data sheet (EDS).

## Slide 4
Product Robustness
Compatible with a broad range of substrates and pretreatments including: CRS, HRS, B1000 DIW, B1000 P99X, Galvanneal Steel, Galvanized Steel, Aluminum, Shot Blast Steel, and Cast Iron
Compatible with multiple PPG Topcoats
Wide application window
Corrosion Resistance
>1,000 hours salt spray resistance (ASTM B117)
>40 cycles with cyclic corrosion resistance (SAE J2334)
Passes various HDE OEM highest level specifications for corrosion
PPG Spectracron VRP Primer Key Attributes
Notes: *Current formulation has passed John Deere Level 1 & 2 specs (240 & 504 hours on B1000 P99X, respectively), it has also met Level 3 specs (1008 hours on B952 P99X) when tested on B1000 P99X instead of B952 P99X. B952 (Zinc Phosphate w/ sealant) is a better performing substrate than B1000 P99X (Iron Phosphate w/ sealant), so it is expected that current formulation will pass John Deere Level 3 specs (panels are currently in test and results should by in by Aug. 31, 2018).
**Previous formulation has passed CAT cyclic and edge specs – only changes are additives (disperserant, rheological additive) and are not expected to impact corrosion performance. In house testing thus far has looked good, samples have been sent to CAT to obtain official approval and should be back by Aug. 31, 2018.

## Slide 5
Regulatory Information
Application Flexibility and Efficiency
Wide application window (tested temperature range: 75 - 95°F (24 - 35°C); tested humidity range: 40 - 80% Relative Humidity)
Baked primer : recoat with topcoat w/o sanding for up to 2 weeks
Primer Ambient : recoat with topcoat w/o sanding for up to 2 weeks
Primer W-o-W + topcoat: recoat primer + topcoat w/o sanding for up to 72 hours (topcoat dependent)
Wet-on-wet application time of 5 minutes for high-gloss and high-DOI finishes
2.8 lbs/gal VOC (less exempts)
Specifically formulated without HAPs content
Specifically formulated without heavy metals
PPG Spectracron VRP Primer Key Attributes
Notes: Bullet 1: Conditions Tested:
- 75F, 40% RH
- 95F, 40% RH
- 95F, 80% RH
Bullet 2: If you apply a coat of VRP primer, then cure, then add a topcoat, then cure, then you can recoat w/o sanding for up to two weeks.
Bullet 3: If you apply a coat of VRP primer, then apply a topcoat w/o first baking (w-o-w), then cure, then you can recoat w/o sanding for up to 3 days, but this very dependent on the topcoat applied.
Bullet 7: RM Inventories:
- AICS = Australia
- DSL = Canada
- IECSC = China
- REACH = European Union
- METI/ENCS = Japan
- KECI = Korea
- NZIoC = New Zealand
- NECSI = Taiwan
- TSCA = United States

## Slide 6: PPG Spectracron VRP Recommended Application Basics
Cure Agent: GXM81800
Blend Ratio By Volume: 4:1
Mixed Solids by Volume: 38.6 +/- 3%
Coverage: 619 ft2 per mil per gallon @ 100% efficiency
Application Methods: Electrostatic, Conventional Air Spray
Sag and Pop Resistance: up to 5 (Dry Film) mils including topcoat (even at high temp, high humidity)
Flash Time: 5 minutes minimum
Oven Temperature: 120-200°F (82°C)
Time at Temperature: 20-60 minutes
Low Cure Options: 140°F (60°C) for 30 minutes or 120°F (49°C) for 60 minutes
Air Dry : VRP Primer air dry capable for touch-up purpose
Notes: Sag Resistance: 3 dry mils = ~8 wet mils
Pop Resistance: Dave Nale has done some preliminary pop resistance testing, but says it is very condition (application method, temperature, topcoat, etc.) dependent. Contact him if data for a specific set of conditions is desired. Application properties have been initially evaluated over a wide range of application methods (Dave Nale & Craig Ihm) but not enough data has been collected yet to conclusively recommend any application methods beyond e-stat and conventional; further testing of application methods has been sidelined due to higher priority projects. The hope is that customer trial data and more testing data will be available by the launch of the VRP topcoat.

## Slide 7: PPG Spectracron VRP application window
VRP Primer has demonstrated a wide application window during multiple applications validation sessions runned in ATLS center in OakCreek.
VRP Primer provides a high solvent popping and sag resistance to the coating system in different temperature and Humidity environment (tested from 75 to 95 °F and 40 to 80 %Rh) even when used Wet on wet with a 5 min Flash-Off prior to top coating.
VRP Primer has shown a capability to provide smooth finish in all these conditions
VRP Primer is seen as the most robust primer in IC SBU 2K primer range by application experts.

## Slide 8: Product Specifications and Performance Properties
Parameters | VRP Epoxy Primer
Colors | Gray and Buff
Pretreatments | Iron Phosphate, Shot Blast, Galvanized, Galvanneal, B1000 DIW, B1000 P99X
Substrates | CRS, HRS, Aluminum, Cast Iron
VOC | 2.8 lbs. / gal. less exempts
Gloss Range @ 60° | > 60
Pot-Life | 4 hours
Specifically formulated without heavy metals | Yes
Shelf Life | Part A: 12 months/ Part B: 12 months
Cure Agent | GXM81800
Weight Solids (Blended) | 60.5% +/- 3%
Volume Solids (Blended) | 38.6 +/- 3%
Recommended Wet Film | 3.6-4.7 mils
Recommended Dry Film | 1.3 – 2.0 mils
Flash time | 5 Minutes Minimum
Parameters | VRP Epoxy Primer
Cure | Follows topcoat bake
Dry to Touch (Air dry @77⁰F) | 3 hours
Dry to Handle (Air dry @77⁰F) | 4 hours
To Recoat w/o Sanding | W-o-W primer + baked topcoat= 72 hours Baked primer + baked topcoat = 2 weeks
Initial Adhesion | 5B
Salt Spray Resistance | 1,000+ hours (≤ 2 mm creep) on B1000 P99X Substrate
Humidity (ASTM D2247) | 1,000+ hours
Mar Resistance | 30 XX MEK
Hardness | 4H Pencil
Impact Resistance | 80 in-lbs Direct; 20 in-lbs Reverse
Conical Mandrel | No cracking
Chemical Resistance | 500 hour diesel, water, oil immersion
Durability | Not tested – Not made for primer-only weathering resistance
Blend Ratio w GXM78880 | 2:1 by volume
TDS of Gray Primer
Notes: Spraying thicker than recommended (TRANS) is fine as long as you stay below 3 dry mil sag limit. Spraying thinner than recommended (Agriculture Equip) will likely work but is not ideal – may compromise performance – best performance is in recommended range.

## Slide 9
Corrosion Testing Over Multiple Substrates
VRP Primer-Only
This data represents PRIMER-ONLY testing
* Red outline = blistering occurred on one panel
ASTM-B117 Salt Spray Corrosion Test
Chart: 500 Hours
| ALUMINUM | SHOT BLAST | B1000 P99X | GALVANIZED | GALVANEAL | CAST IRON | B1000 DIW | HRS | CRS
500 Hours | 0 | 0 | 0.53429 | 1.1021 | 1.5025 | 0 | 2.2511 | 3.32 | 3.6436
Chart: 1000 Hours
| ALUMINUM | SHOT BLAST | B1000 P99X | GALVANIZED | GALVANEAL | CAST IRON | B1000 DIW | HRS | CRS
1000 Hours | 0.59143 | 0.337 | 1.7732 | 2.0543 | 4.8 | 0.095 | 2.7168 | 4.1229 | 0
Chart: 1500 Hours
| ALUMINUM | SHOT BLAST | B1000 P99X | GALVANIZED | GALVANEAL | CAST IRON | B1000 DIW | HRS | CRS
1500 Hours | 0.01 | 0.3 | 1.95 | 3.335 | 6.7 | 0 | 0 | 0 | 0
Chart: 2000 Hours
| ALUMINUM | SHOT BLAST | B1000 P99X | GALVANIZED | GALVANEAL | CAST IRON | B1000 DIW | HRS | CRS
 | 0 | 2.29 | 0 | 0 | 0 | 2.95 | 0 | 0 | 0
Good Results Even On Metal Cleaned Only (CRS) at 500H = Worst Case Scenario
Failure
Notes: CRS and HRS were both bare (cleaned, but not treated beyond that), so poor performance was expected.
B1000 DIW, CRS, HRS not tested at 1500 hrs as these were deemed “weaker” substrates and thus not expected to perform well at 1500 hours.
CRS failure at 1000 hours indicates that so much paint scraped off panel that it was not worth measuring scribe creep as it would be unacceptable to any OEM.
Galvaneal primer-only performance not great at 1000 and 1500 hrs, but performed quite well w/ topcoat as is shown later in presentation
Contact Dave Nale (Oak Creek COE) if photos of primer only salt spray are needed

## Slide 10: Cyclic Corrosion & Edge Protection Testing Primer-Only
SAE J2334 Cyclic Corrosion Testing Results

## Slide 11
Corrosion Testing Over Multiple Substrates
VRP Primer + PPG Topcoats
ASTM-B117 Salt Spray Corrosion Test
VRP Primer + Topcoat
500 Hours
Salt spray performance across wide range of substrates
Demonstrated compatibility with wide range of topcoats
Chart: Average Creep (mm)
| Black | Yellow | Red | White | Green
ALUMINUM | 0 | 0 | 0 | 0
B1000 DIW | 3.5725 | 2.2432 | 2.5471 | 2.2036 | 2.4679
B1000 P99X | 1.4061 | 0.69821 | 0.65393 | 0.70679 | 0.43821
CAST IRON | 0 | 0 | 0 | 0 | 0
CRS | 1.2146 | 1.9071 | 2.5096 | 2.2196 | 2.7475
GALVANNEAL | 0.37536 | 0.36536 | 0 | 2.2868 | 0
GALVANIZED | 0 | 0.80214 | 3.0525 | 0
HRS | 2.2732 | 1.7946 | 1.3557 | 1.5532 | 2.1296
SHOT BLAST | 1.3305 | 0.675 | 0.2785 | 0.1735 | 0.8315
ALUMINUM*
Notes: While corrosion protection goes down w/ HSX series, VRP is still very compatible with it – testing was done w/ 10 minute wet-on-wet and it is hypothesized that corrosion performance could increase with longer dry times (longer dry times are typical for TRANS, where HSX series is used).

## Slide 12
Chart: Average Creep (mm)
| Black | Yellow | Red | White | Green
ALUMINUM | 0.88393 | 0.19821 | 0.24036 | 0.405 | 0.34
B1000 DIW | 5.6429 | 3.8875 | 4.4918 | 3.9557 | 3.4293
B1000 P99X | 2.6361 | 1.5832 | 1.51 | 1.4646 | 1.7911
CAST IRON | 0.22179 | 0.043214 | 1.1743 | 0.74571 | 0.0975
CRS | 3.4189 | 3.5046 | 5.6186 | 5.675 | 3.4818
GALVANNEAL | 2.5389 | 2.0511 | 2.0011 | 0.20357 | 1.7914
GALVANIZED | 0.048929 | 0.024643 | 0.1 | 0.65036 | 0.0028571
HRS | 2.9857 | 2.2261 | 2.2914 | 3.5782 | 2.9789
SHOT BLAST | 3.279 | 1.653 | 0.361 | 0.6215 | 0.279
Corrosion Testing Over Multiple Substrates
VRP Primer + PPG Topcoats
ASTM-B117 Salt Spray Corrosion Test
VRP Primer + Topcoat
1000 Hours
Overpassing industry salt spray requirement on multiple substrates
Notes: While corrosion protection goes down w/ HSX series, VRP is still very compatible with it – testing was done w/ 10 minute wet-on-wet and it is hypothesized that corrosion performance could increase with longer dry times.
Again, HRS & CRS were bare (no treatment besides cleaning), represents absolute worst case scenario.
Black = HSX939606, Yellow = SPU78367, Red = SPU65250B, White = HSL919071, Green = SPU77777

## Slide 13
Corrosion Testing Over Multiple Substrates
VRP Primer + PPG Topcoats
ASTM-B117 Salt Spray Corrosion Test
VRP Primer + Topcoat
1500 Hours
Chart: Average Creep (mm)
| Black | Yellow | Red | White | Green
ALUMINUM | 0.26821 | 0.56464 | 0.53679 | 0 | 0.47679
B1000 P99X | 4.2507 | 2.3993 | 1.7039 | 2.97 | 2.8639
GALVANNEAL | 2.9646 | 2.0807 | 2.4764 | 3.9289 | 1.9475
GALVANIZED | 0.6975 | 0.028571 | 0.565 | 1.335 | 0.081786
SHOT BLAST | 1.461 | 1.558 | 1.0375 | 0.7585 | 0.2585
Notes: CRS, HRS, B1000 DIW not tested at 1500 hours as they were not expected to perform at an acceptable level
While corrosion protection goes down w/ HSX series, VRP is still very compatible with it – testing was done w/ 10 minute wet-on-wet and it is hypothesized that corrosion performance could increase with longer dry times.
Black = HSX939606, Yellow = SPU78367, Red = SPU65250B, White = HSL919071, Green = SPU77777

## Slide 14
Corrosion Testing Over Multiple Substrates
VRP Primer + PPG Topcoats
ASTM-B117 Salt Spray Corrosion Test
VRP Primer + Topcoat
2000 Hours
Chart: Average Creep (mm)
| Black | Yellow | Red | White | Green
CAST IRON | 0.77643 | 0.65214 | 1.0986 | 0.9 | 0.11929
SHOT BLAST | 0.7705 | 0.795 | 1.417 | 0.9605 | 0.7025
Notes: Black = HSX939606, Yellow = SPU78367, Red = SPU65250B, White = HSL919071, Green = SPU77777

## Slide 15: ASTM-B117 1000 Hour Salt Spray: Cold & Hot Rolled Steel
Cold Rolled Steel
(no pretreatment)
Hot Rolled Steel
(no pretreatment)
Notes: 500 hours photo on sharepoint

## Slide 16: ASTM-B117 1000 Hour Salt Spray: B1000 DIW & B1000 P99X
B1000 DIW
Iron Phosphate + Water rinse
B1000 P99X
Iron Phosphate + Non Chrome sealer

## Slide 17: ASTM-B117 1000 Hour Salt Spray: Galvanized & Galvanneal Steel
Galvanized Steel
Galvanneal Steel

## Slide 18: ASTM-B117 1000 Hour Salt Spray: Shot Blast Steel

## Slide 19: ASTM-B117 1000 Hour Salt Spray: Cast Iron
Poor appearance due to high profile surface of customer cast iron panels

## Slide 20: ASTM-B117 1000 Hour Salt Spray: Aluminum

## Slide 21: Color Pallet Capability
VRP Primer can be tinted on demand by tinter addition and achieve a wide range of colors.
This opens new opportunity where multiple primer colors is required
Solution when a colored primer is used on hidden parts with no topcoat*
* Not to be used in areas in direct contact with UV

## Slide 22: Selling PPG Spectracron VRP Primer Key Value Points for Customers
Looking for a primer that will work for all your parts and with all your different manufacturing processes and tier supplier and outsourcers? PPG Spectracron VRP primer’s proven compatibility with a broad range of substrates and topcoats as well as its application flexibility make it the ideal single source solution for all your industrial manufacturing primer needs.
Looking to prevent premature rusting and increase the lifespan of your product? PPG Spectracron VRP primer satisfies various HDE OEM’s highest level specification for corrosion resistance and edge protection while equaling or outperforming other high performance primers in corrosion prevention.
Want to improve efficiency on your shop floor? Speed up application time? With the ability for 5 minute wet-on-wet application, PPG Spectracron VRP primer can greatly reduce downtime between primer and topcoat application, allowing for faster production.
Trying to reduce emissions and move towards a more sustainable future? With only 2.8 lbs/gal VOC (less exemptions) and specifically formulated without HAPs, PPG Spectracron VRP primer delivers exceptional performance with minimal environmental impact.
Notes: Bullet 1: Especially good for jobcoaters who have to coat multiple parts for different OEMs  one stop shop

## Slide 23
Notes: Questions