## Slide 1: Spectracron® VRPPE
Solventborne Primer
Availability | Technology | Coating Type | Chemistry | Substrates
USCA – MTO | Liquid Solventborne | Primer | 2K Epoxy | CRS, HRS, Galvaneal Steel, Galvanized Steel, Aluminum, Shot Blast Steel and Cast Iron
PPG Segments
Agriculture and Construction Equipment
Transportation
General Industrial
Suggested Uses
Agriculture Equipment
Construction Equipment
Material Handling
Recreational Vehicles
Truck Bodies and Beds
Electrical
Features | Potential Customer Benefits
Strong corrosion performance | Protects assets and increases product longevity
Multi-metal compatibility | Reduces process complexity, footprint and costs
Excellent pop and sag performance | Lowers application cost and rework
Wide application and recoat window | Provides flexibility in process conditions
Wet-on-wet capable | Increases throughput and decreases process cost
Customizable colors | Allows differentiation through color
2.8 lbs./gal. VOCs, less exempts and specifically formulated without HAPs | Reduces cost related to environmental controls
Initially introduced into the OEM agriculture and construction equipment segment this primer technology has demonstrated value to our customers.

## Slide 2: Spectracron® VRPPE
Solventborne Primer
Product Characteristics* |  | 
Color | - | Gray & Buff, tintable
Gloss at 60º | ASTM D523 | > 60
VOCs | - | 2.8 lbs./gal. (336 g/L), less exempts
Cure | - | Oven Time/Temp: 20-60 min @ 120-200°F Wet on Wet: 5 min flash, topcoat bake
Performance Properties* |  | 
Pencil Hardness | ASTM D3363 | 4H
Conical Mandrel Bend | ASTM D522 | 1/8”
Impact Resistance, Direct / Reverse | ASTM D2794 | 80 / 20 in-lbs
Chemical Resistance (diesel, water, oil immersion) | ASTM D1308 | 500 hours
Humidity Resistance | ASTM D2247 | 1,000 hours
Salt Spray Resistance | ASTM B117 | >1,000 hours
Cyclic Corrosion Resistance | SAE J2334 | >40 cycles
Compatible Products
Topcoats: Spectracron SPU77777, Spectracron SPU79367, Spectracron SPU65250B, Spectracron HSI, Spectracron HSL, Spectracron VRPT
*results obtained over iron phosphate pretreated CRS panels. Salt spray performance dependent on pretreatment used.
Key Features
Strong corrosion performance
Multi-metal compatibility
Excellent pop and sag performance
Wide application and recoat window
*For specific product VOC information refer to the environmental data sheet (EDS).

## Slide 3: Spectracron® VRPP
Solventborne Primer
Transmission and distribution
Agriculture equipment
Construction equipment and
waste containers
Additional end-use photos