## Slide 1: DURASTAR® Extrusion Coatings
Availability | Technology | Coating Type | Chemistry | Substrates
USCA | Liquid Solventborne | Topcoat | Polyester | Aluminum
PPG Segments
Architectural Building Products
Aluminum Extrusions
Suggested Uses
Plate Aluminum
Brake Metal
Store Fronts
Features | Potential Customer Benefits
One coat system | Increases throughput and reduces process cost
Full solid color palette | Allows for design differentiation
Primer compatible | Increase protection in sea coast environments
Hard finish | Offers durability during handling, installation and can be used in high-traffic areas
Value engineered | Offers economical performance
Low cure temperature | Reduces energy consumption and process costs
One or two coat spray-applied solventborne ultradurale polyester coating system.
Meets FGIA/AAMA 2604 specifications
Notes: http://www.ppgmetalcoatings.com/getmedia/8a4c8590-9cf7-46d5-95f6-1a85fb3aaa34/Polycron.pdf.aspx
VOC:
UC108921 2.58 lbs/gal
UC114638 2.53 lbs/gal

## Slide 2
DURASTAR® Extrusion Coatings
Meets FGIA/AAMA 2604 specifications
Specifications |  | 
Colors Available1 |  | A wide range of solid colors
Dry Film Thickness | ASTM D1400 | 1.0 - 1.2 mils color topcoat
Gloss | ASTM D523 @ 60° | High, medium and low gloss
Pencil Hardness | ASTM D3363 | H - 2H
Cross Hatch Adhesion | ASTM D3359, 1/16” dry, wet & boiling water | Pass – no removal of film under tape
Direct Impact | ASTM D5420 3mm distortion | Pass – no removal of film from substrate
Abrasion – Sand Falling | ASTM D968 | Pass – abrasion coefficient > 20 liters/mil
Acid Resistance | ASTM D1308 10% muriatic acid spot test | 15 minutes – No attack
Alkali Resistance | Mortar pat test 100% relative humidity @ 100°F (38° C) | 24 hours – No attack
Detergent Resistance | ASTM D2248, 3% immersion @ 100°F (38° C) | 72 hours – No attack
Salt Spray Resistance3 | ASTM B117, 3000 hrs. 5% NaCl @ 100° F (38° C) | 1/16” maximum undercutting
Humidity Resistance | ASTM D714 ASTM D2247, 3000 hrs. 100% relative humidity @ 100°F (38° C) | Up to few #8 blisters maximum
Exterior Exposure | ASTM G7/G7M 5 yrs. @ 45°, south Florida Film Integrity Gloss Retention | ASTM D2244 / ASTM D4214 Maximum 5 fade / minimum 8 chalk Very Good Greater than 30%
1 The range of color availability will vary depending upon exposure requirements and architect specifications
2 For more critical applications, a primer/topcoat system and greater film thicknesses may be recommended. Consult PPG specialists for recommendation when developing specifications.
3 Corrosion performance is dependent on properly cleaned and pretreated substrate
These test results are based on methods believed to be correct and were performed on laboratory prepared panels. This document is not a guarantee of future performance.
Key Features
Full color pallet
Hard Finish
Value Engineered
One coat system
Notes: AAMA 2603