## Slide 1: PPG PRIMERON® High-performance powder primer series
July 18, 2024

## Slide 2: Why use a powder primer?
After blasting the metal surfaces, primers can be applied to slow down the speed of oxidation, create more consistency in the application of the powder coatings and allow the powder coatings to more easily bond to metal edges.

## Slide 3: PPG powder primers are designed to meet various ISO 12944 corrosivity category standards
Category and Typical Environment |  | 
 | C1 | Indoor: Heated indoor spaces without elevated condensation.
 | C2 | Indoor: Unheated indoor spaces with increased condensation. Outdoor: Atmospheres with low level of pollution. Mainly rural areas.
 | C3 | Indoor: Production rooms with high humidity and low contamination. Outdoor: Urban and industrial atmospheres with moderate sulfur dioxide pollution. Coastal areas with low salinity.
 | C4 | Indoor: chemical facilities, swimming pools. Outdoor: Industrial areas and coastal areas with moderate salinity.
 | C5 | Indoor: Buildings with almost permanent condensation and heavy air pollution. Outdoor: Industrial areas with high humidity and aggressive atmosphere.
 | CX | Outdoor: Coastal and offshore areas with high salinity and industrial areas with extreme humidity.
MOST SEVERE
LEAST SEVERE

## Slide 4: Introducing the PPG Primeron primer portfolio
Five product lines designed with special features that meet various substrate, environmental and end-use requirements
Provides high corrosion resistance for a variety of substrates, including steel, hot-dip-galvanized steel, metalized steel and aluminum
Suggested end uses
Gas or liquid tanks and pipelines
Truck, trailer and automotive parts
Agricultural and construction machinery
Automotive underbody and other parts
Seacoast or applications with high corrosion performance requirements

## Slide 5: Primeron high-performance product lines
MOST SEVERE
LEAST SEVERE
A traditional zinc-rich primer offering our best corrosion protection in this technology
A zinc-rich primer that delivers exceptional corrosion protection and a balanced offering of other properties
Designed for layered protection in automotive specialty markets, with options for exceptional flexibility, chip and corrosion resistance, UV durability and outgassing
High-edge primer technology offering best-in-class corrosion protection for substrates with sharp and laser-cut edges
Outgas-friendly, zinc-alternative primers that provide very excellent corrosion protection for multiple substrates
Primeron Legacy
Primeron Optimal
Primeron Auto
Primeron Edge
Primeron Versa

## Slide 6
Zinc-rich primer with exceptional corrosion protection
Suggested Industries
Energy applications
General industrial
Automotive parts and accessories
Products, benefits and characteristics
PCM70140: A traditional zinc-rich primer offering our best corrosion protection in this technology
Suggested End Uses
Gas or liquid tanks and pipelines
Seacoast walls, fences or metal objects
ISO 12944 Corrosivity Category
C5
Corrosion performance
on mechanically pretreated steel
Very good flow and appearance
Low bake capability

## Slide 7
Partial Curing | 
7 - 10 minutes | 275˚ F (135˚ C)
3 - 5 minutes | 300˚ F (149˚ C)
1 - 2 minutes | 350˚ F (177˚ C)
Storage Conditions
12 months / 86˚ F (30˚ C)
Full Curing | 
20 minutes | 275˚ F (135˚ C)
10 minutes | 300˚ F (149˚ C)
5 minutes | 350˚ F (177˚ C)
Properties | Test Method | Value
Color | - | Dark gray
Surface | - | Semi-gloss, smooth
Gloss at 60° | ISO 2813 | 55-70
Specific Gravity | Calculated | 3.6 g/cm3
Impact Resistance | ISO 6272 / ASTM D2794 | 80 in./lbs. direct 80 in./lbs. reverse
Adhesion | ISO 2409 | 5B, pass
Conical Mandrel | ISO 6860 | 1/8”, pass
Zinc-rich primer with exceptional corrosion protection

## Slide 8
Zinc-rich primer with balanced performance properties
Suggested Industries
Heavy-duty equipment
General industrial
Automotive parts and accessories
Corrosion performance
on all substrates
Recoatable with higher transfer efficiency than traditional zinc primers
Almost double the theoretical coverage of Primeron Legacy primer
Suggested End Uses
Construction/agricultural equipment
Seacoast walls, fences or metal objects
ISO 12944 Corrosivity Category
C5
2x
Products, benefits and characteristics
PCMT70149: Exceptional corrosion resistance and a balanced offering of other properties, including better coverage, applied cost, adhesion, semi-conductivity, recoatability and transfer efficiency than traditional zinc primers

## Slide 9
Partial Curing | 
7 - 10 minutes | 275˚ F (135˚ C)
3 - 5 minutes | 300˚ F (149˚ C)
1 - 2 minutes | 350˚ F (177˚ C)
Storage Conditions
12 months / 86˚ F (30˚ C)
Full Curing | 
20 minutes | 275˚ F (135˚ C)
10 minutes | 300˚ F (149˚ C)
5 minutes | 350˚ F (177˚ C)
Properties | Test Method | Value
Color | - | Dark gray
Surface | - | Semi-gloss, smooth
Gloss at 60° | ISO 2813 | 55-70
Specific Gravity | Calculated | 2.0 g/cm3
Impact Resistance | ISO 6272 / ASTM D2794 | 160 in./lbs. direct
Adhesion | ISO 2409 | 5B, pass
Conical Mandrel | ISO 6860 | 1/8”, pass
Zinc-rich primer with balanced performance properties

## Slide 10
Layered protection for automotive and specialty markets
Suggested Industries
Automotive parts and accessories
Products, benefits and characteristics
PCF90202, PCF70406: polyester epoxy primers for aluminum wheels with great adhesion to liquid topcoats and excellent outgassing
PCT99157: UV-durable polyester primer for aluminum wheels with great adhesion to liquid topcoats and excellent outgassing
PCM90133: epoxy primer for steel/aluminum underbody applications with excellent performance over electrocoat or used as a monocoat
PCF70404: polyester epoxy primer for steel/aluminum with excellent chip resistance when used over electrocoat
PCT90111M: multi-use, polyester primer optimized for alkyd topcoats
Suggested End Uses
Aluminum wheels
Automotive underbody parts
Automotive body
ISO 12944 Corrosivity Category
C4: PCM90133
C3: All other products
Excellent layering over e-coat or under liquid topcoats
Good flow, appearance and mechanical properties
Options for chip resistance, UV durability and outgassing

## Slide 11
Properties* | PCF90202 | PCF70406 | PCT99157 | PCM90133 | PCF70404 | PCT9011M
Color | Black | Gray | Black | Black | Gray | Black
Surface | Smooth | Smooth | Smooth | Smooth | Smooth | Smooth
Gloss at 60° | 70 minimum | 70 minimum | 80 minimum | 80 minimum | 10-25 | 55-70
Specific Gravity | 1.3 g/cm3 | 1.3 g/cm3 | 1.2 g/cm3 | 1.5 g/cm3 | 1.3 g/cm3 | 1.6 g/cm3
Impact Resistance | 100 in./lbs. direct | 100 in./lbs. direct | 80 in./lbs. direct | 160 in./lbs. direct | 100 in./lbs. direct | 80 in./lbs. direct
Adhesion | 5B, pass | 5B, pass | 5B, pass | 5B, pass | 5B, pass | 5B, pass
Conical Mandrel | 1/8”, pass | 1/8”, pass | 1/8”, pass | 1/8”, pass | 1/8”, pass | 1/8”, pass
Full Curing | 20 minutes 350˚ F (177˚ C) | 30 minutes 350˚ F (177˚ C) | 30 minutes 350˚ F (177˚ C) | 5 minutes 350˚ F (177˚ C) | 30 minutes 350˚ F (177˚ C) | 25 minutes 350˚ F (177˚ C)
* Properties on this slide use the same test methods as other Primeron products. For information about full curing at other temperatures, partial curing or storage conditions, please contact your PPG sales representative or email ic-na@ppg.com.
Layered protection for automotive and specialty markets

## Slide 12
Designed for best-in-class sharp edge protection
Suggested Industries
Heavy-duty equipment
Electrical and power generation
Strong corrosion protection
Enhanced edge coverage for sharp, complex or laser-cut parts
Can help eliminate edge rounding equipment / extra machining
Suggested End Uses
Vents, steps and louvres
Electrical boxes and air conditioners
ISO 12944 Corrosivity Category
C4: PCMT30105
C3: PCF70283
Products, benefits and characteristics
PCF70283: A preferred primer for heavy-duty equipment, offering good edge corrosion resistance and overall protection
PCMT30105: A semi-conductive product that allows for easier topcoating and provides excellent sharp edge protection

## Slide 13
Storage Conditions
12 - 24 months / 86˚ F (30˚ C)
Properties | Test Method | Value*
Color | - | Medium gray (PCF70283) Light tan (PCMT30105)
Surface | - | Smooth
Gloss at 60° | ISO 2813 | Varies by product
Specific Gravity | Calculated | 1.6 g/cm3
Impact Resistance | ISO 6272 / ASTM D2794 | 80 in./lbs. direct
Adhesion | ASTM D3359 | 5B, pass
Conical Mandrel | ASTM D522 | 1/8”, pass
* Values indicate a range of performance across the entire family of products. For product-specific values, please contact your PPG sales representative or email ic-na@ppg.com.
Designed for best-in-class sharp edge protection
Partial Curing* | 
5 - 7 minutes | 350˚ F (177˚ C)
4 - 5 minutes | 375˚ F (191˚ C)
3 - 4 minutes | 400˚ F (204˚ C)
Full Curing* | 
16 - 20 minutes | 350˚ F (177˚ C)
12 - 15 minutes | 375˚ F (191˚ C)
8 - 12 minutes | 400˚ F (204˚ C)

## Slide 14
A versatile primer for multi-substrate use
Suggested Industries
Electrical and power generation
General industrial
Strong corrosion protection across a broad range of substrates
Good intercoat adhesion and compatibility with a wide range of topcoats
Excellent alternatives to zinc-rich primers
Suggested End Uses
Fencing, utility poles, lamp posts
Stadium seating
ISO 12944 Corrosivity Category
C5: PCMT70101
C4: PCMB70102
Products, benefits and characteristics
PCMT70101: Surface-tolerant epoxy primer that has good adhesion, great coverage and easy application with semi-conductivity that facilitates topcoat application
PCMB70102: A user-friendly epoxy primer that can adapt to many different applications; especially outgas-friendly when used over galvanized steel and cast metals
Zn

## Slide 15
Storage Conditions
12 months / 86˚ F (30˚ C)
Properties | Test Method | Value*
Color | - | Gray
Surface | - | Smooth
Gloss at 60° | ISO 2813 | Varies by product
Specific Gravity | Calculated | 1.6 g/cm3
Impact Resistance | ISO 6272 / ASTM D2794 | 80 in./lbs. direct
Adhesion | ASTM D3359 | 5B, pass
Conical Mandrel | ASTM D522 | 1/8”, pass
* Values indicate a range of performance across the entire family of products. For product-specific values, please contact your PPG sales representative or email ic-na@ppg.com.
A versatile primer for multi-substrate use
Partial Curing* | 
6 - 9 minutes | 275˚ F (135˚ C)
3 - 5 minutes | 300˚ F (149˚ C)
2 - 3 minutes | 350˚ F (177˚ C)
Full Curing* | 
20 - 30 minutes | 275˚ F (135˚ C)
10 - 20 minutes | 300˚ F (149˚ C)
5 - 10 minutes | 350˚ F (177˚ C)

## Slide 16: Primeron primers key feature summary
 | Primeron Legacy | Primeron Optimal | Primeron Auto* | Primeron Edge* | Primeron Versa*
Key Features | Zinc primer offering our best corrosion protection in this technology | Zinc-rich primer with excellent corrosion protection and a balance of other properties | Layer with liquid topcoats or over e-coat for automotive-grade performance | Very good sharp edge coverage, hides casting defects | Multi-substrate capable, good intercoat adhesion, excellent alternative to zinc
Chemistry | Epoxy | Epoxy | Epoxy, polyester, polyester epoxy | Epoxy, polyester epoxy | Epoxy
Density | 3.6 g/cm3 | 2.0 g/cm3 | 1.7 g/cm3 | 1.6 g/cm3 | 1.6 g/cm3
Overall Corrosion Performance | ★★★★ | ★★★★ | ★★★ | ★★★ | ★★★★
Edge Protection | ★ | ★★★ | ★★ | ★★★ | ★★
Mechanical Properties | ★★ | ★★ | ★★★ | ★★ | ★★
Coverage | ★ | ★★ | ★★ | ★★★ | ★★★
* Values indicate a range of performance across the entire family of products. For product-specific values, please contact your PPG sales representative or email ic-na@ppg.com.

## Slide 17: Thank you for your time today
Your Name Here Your Title
O: 123-456-7890 M: 123-456-7890 yourname@ppg.com