## Slide 1: Spectracron® HSL
Solventborne Topcoat
Availability | Technology | Coating Type | Chemistry | Substrates
USCA – Stock & MTO | Liquid Solventborne | Topcoat | 2K Polyurethane | The substrate has to be primed: CRS, Galvaneal Steel, Galvanized Steel, Aluminum, Blasted Steel and Cast Iron
 |  |  |  | Adhesion promotor required: Plastics: TPO, ABS, Nylon
PPG Segments
Agriculture and Construction
General Industrial
Transportation
Suggested Uses
Boats
Equipment and Man Lifts
Generators
Locomotives
School Buses
Truck Bodies and Beds
Features | Potential Customer Benefits
Lower cost topcoat | Offers economical performance
Wide gloss range | Tailors final finish to customer requirement
Metallic color palette | Allows differentiation through color
Onsite mix line capable | Increases responsiveness on color
Customizable colors as low as 5 gallons | Reduces inventory and hazmat costs
Wet-on-wet capable | Increases throughput and decreases process cost
Specifically formulated without HAPs | Reduces cost related to environmental controls
Initially introduced into the transportation segment this basecoat technology has demonstrated value to our customers.

## Slide 2
Product Characteristics* |  | 
Color | - | Solid and Metallic
Gloss at 60º | ASTM D523 | Solid: 5-90 Metallic: >70
VOCs | - | ≤ 3.9 lbs./gal. (≤ 467 g/L), less exempts
Cure | - | Oven Time/Temp: 20-60 min @ 120-180°F
Wet on wet time | - | 5 - 10 min
Performance Properties* |  | 
Pencil Hardness | ASTM D3363 | 2H
Conical Mandrel Bend | ASTM D522 | 1/8”
Adhesion | ASTM D3359 | 5B
Humidity Resistance | ASTM D2247 | 1000 hours
Weatherometer | SAE J2527 ASTM G155-05A | 1000 hours
Compatible Products
Primers: Liquid - Spectracron W43181A, PRU, SEP78278, SEP78284, SEP80613, SEP76001, SEP83052, VRPPE
*results obtained over primed iron phosphate pretreated CRS panels.
Key Features
Lower cost topcoat
Wide gloss range
Metallic color palette
Onsite mix line capable
Spectracron® HSL
Solventborne Topcoat
*Excess film thickness will retard dry times. Do not apply at temperatures below 50°F(10°C). For specific product VOC information refer to the environmental data sheet (EDS).