## Slide 1: VersolonTM ALK-200 Series
Solventborne Topcoats
Availability | Technology | Coating Type | Chemistry | Substrates
USCA – MTO | Liquid Solventborne | Topcoat | 1K Alkyd Acrylic | Blasted Steel, Cold Rolled Steel, Hot Rolled Steel and Aluminum
PPG Segments
Agriculture and Construction Equipment
General Industrial
Suggested Uses
Agricultural Equipment
Construction Equipment
Fabricated Metal
Furniture
Industrial Equipment
Material Handling
Structural Steel
Telecommunications
Features | Potential Customer Benefits
Low-cost topcoat | Offers economical performance
Fast drying | Lowers cost and increases throughput
One component | Ready to spray, reduces production time
Low to high gloss range | Tailors final finish to customer requirement
Excellent flow and leveling | Ease of application
Acrylic modified to improve exterior durability | Protects and retains product appearance
Customizable colors as low as 1 gallon | Reduces inventory and hazmat costs
This versatile solvent-based topcoat is found across a variety of industries and end uses.

## Slide 2: VersolonTM ALK-200 Series
Solventborne Topcoats
Product Characteristics* |  | 
Color | - | Multiple
Gloss at 60º | ASTM D523 | 20 - 90
VOCs | - | 5.0 lbs./gal. (600 g/L)
Cure | - | Oven Time/Temp: 20-30 min @ 180°F (82°C) Air Dry: To Touch: 15-30 min To Handle: 1-2 hrs
Performance Properties* |  | 
Pencil Hardness | ASTM D3363 | HB - H
Conical Mandrel Bend | ASTM D522 | 1/8”
Adhesion | ASTM D3359 | 5B
Humidity Resistance | ASTM D2247 | 300 Hours
Weatherometer | SAE J2527 ASTM G155-05A | 750 Hours
Compatible Products
Primers: Versolon NLP-908, NLP-X95, NLP-495, NLP-795, NLP-951, NLP-X35, NLP-435, and NLP-935 and Spectracron® W43181A
*results obtained over iron phosphate pretreatment with primer on CRS panels. Performance dependent on pretreatment and primer used.
Key Features
Low-cost topcoat
Low to high gloss range
Fast drying
One component
*Excess film thickness will retard dry times and affect the recoat window. Do not apply at temperatures below 50°F(10°C). For specific product VOC information refer to the environmental data sheet (EDS).
Notes: Online at CAT