## Slide 1: VersolonTM AUE-370 Series
Solventborne Topcoats / Direct To Metal
Availability | Technology | Coating Type | Chemistry | Substrates
USCA – MTO / Stock | Liquid Solventborne | Topcoat Direct To Metal | 2K Polyurethane | Direct to Metal Blasted, cold rolled and hot rolled steel, aluminum, galvanized, plastics*, fiberglass* Substrate has to be primed: Galvanneal, plastics, fiberglass
PPG Segments
Agriculture and Construction Equipment
General Industrial
Suggested Uses
Building Materials
Heavy Duty Equipment
Industrial Equipment
Material Handling
Telecommunications
Features | Potential Customer Benefits
High build capable | Lowers application costs and rework
Excellent abrasion and mar resistance | Reduces damage in handling and assembly
Strong durability performance | Protects and retains product appearance
High solids formulation | Lower applied costs
Wide color palette | Allows differentiation through color
Corrosion and durability in one layer | Lowers cost and increases throughput
Customizable colors as low as 1 gallon | Reduces inventory and hazmat costs
This versatile solvent-based topcoat is found across a variety of industries and end uses.
*Due to the variability in plastic and fiberglass substrates, it’s highly recommended to test adhesion on a small sample before application.

## Slide 2: VersolonTM AUE-370 Series
Solventborne Topcoats / Direct To Metal
Product Characteristics* |  | 
Color | - | Multiple
Gloss at 60º | ASTM D523 | 85 - 95
VOCs | - | ≤3.6 lbs./gal. (431 g/L)
Solids % by volume |  | 60.5 ± 3.0
Cure | - | Oven Time/Temp: 20 - 30 min up to 180°F (82°C) Air Dry: To Touch: 3-5 hrs To Handle: 8-12 hrs
Performance Properties* |  | 
Pencil Hardness | ASTM D3363 | H – 2H
Conical Mandrel Bend | ASTM D522 | 1/8”
Adhesion | ASTM D3359 | 5B
Abrasion/Mar Resistance | ASTM 4060 | <100mg loss
Humidity Resistance | ASTM D2247 | >1000 Hours
Salt Spray Resistance | ASTM B117 | 500 - 1000 Hours
Weatherometer | SAE J2527 ASTM G155-05A | 600 Hours
Compatible Products
Primers: Versolon HSP385, HBE-400 & EXP-591 series and Spectracron® W43181A
*results obtained over iron phosphate pretreatment with primer on CRS panels. Performance dependent on pretreatment and primer used.
Key Features
High build capable
High solids formulation
Excellent abrasion and mar resistance
Strong durability performance
*Excess film thickness will retard dry times and effect recoat window. Do not apply at temperatures below 40°F(4°C). For specific product VOC information refer to the environmental data sheet (EDS).
Notes: Online at CAT