## Slide 1: Spectracron® SEP
Solventborne Primer – SEP78278, SEP78284, SEP80613
Availability | Technology | Coating Type | Chemistry | Substrates
USCA – MTO | Liquid Solventborne | Primer | 2K Epoxy | CRS, Galvaneal Steel, Galvanized Steel, Aluminum, Blasted Steel and Cast Iron
PPG Segments
Transportation
Suggested Uses
Truck Bodies and Beds
Refuse Trucks
Concrete Mixers
Truck Trailer
Features | Potential Customer Benefits
Class A appearance | Meets stringent appearance requirements
Multi-metal compatibility | Reduces process complexity, footprint and costs
Wide application window | Provides flexibility in process conditions
Excellent pop and sag performance | Lowers application cost and rework
Wet-on-wet capable | Increases throughput and decreases process cost
Extended pot life | Increases throughput and decreases process cost
Initially introduced into the transportation segment this primer technology has demonstrated value to our customers.

## Slide 2
Product Characteristics |  | 
Color | - | Gray and Buff
Gloss at 60º | ASTM D523 | 50 - 70
VOCs | - | ≤ 3.36 lbs./gal. (≤ 403 g/L)
Cure | - | Oven Time/Temp: 30-60 min @ 120-150°F Air Dry*: To Touch: 30 min To Handle: 4 hrs
Performance Properties* |  | 
Conical Mandrel Bend | ASTM D522 | 1/8”
Adhesion | ASTM D3359 | 5B
Impact Resistance - Direct | ASTM D2794 | 160 in-lbs
Pot Life |  | 4+ hours
Humidity Resistance | ASTM D2247 | 1,000 hours
Salt Spray Resistance | ASTM B117 | 1,000 hours
Cyclic Corrosion | SAE J2334 | 40 cycles
Compatible Products
Topcoats: Spectracron HSB, HSS, HSL, HSI, HST and HSU series
*results obtained over iron phosphate pretreated CRS panels. Salt spray and cyclic corrosion performance dependent on pretreatment used.
Key Features
Class A appearance
Multi-metal compatibility
Wide application window
Extended pot life
Spectracron® SEP
Solventborne Primer – SEP78278, SEP78284, SEP80613
*Excess film thickness will retard dry times. Do not apply at temperatures below 50°F(10°C).

## Slide 3
Truck Bodies
Refuse Trucks
Concrete Mixers
Additional end-use photos
Spectracron® SEP
Solventborne Primer – SEP78278, SEP78284, SEP80613
Truck Trailer