## Slide 1: Spectracron® HST
Solventborne Topcoat
Availability | Technology | Coating Type | Chemistry | Substrates
USCA – MTO | Liquid Solventborne | Topcoat | 2K Polyurethane | The substrate has to be primed: Colded Rolled Steel, Galvaneal Steel, Galvanized Steel, Aluminum, Blasted Steel and Cast Iron
 |  |  |  | Adhesion promotor required: Plastics: TPO, ABS, Nylon
PPG Segments
Transportation
Suggested Uses
Truck Bodies and Beds
Refuse Trucks
Concrete Mixers
Recreation Vehicles
Features | Potential Customer Benefits
Metallic color palette | Allows differentiation through color
Wide application window | Provides flexibility in process conditions
Onsite mix line capable | Increases responsiveness on color
Class A appearance | Meets stringent appearance requirements
Wet-on-wet capable | Increases throughput and decreases process cost
Customizable colors as low as 5 gallons | Reduces inventory and hazmat costs
≤3.6 lbs/gal VOCs and specifically formulated without HAPs | Reduces cost related to environmental controls
Initially introduced into the transportation segment this basecoat technology has demonstrated value to our customers.

## Slide 2
Product Characteristics* |  | 
Color | - | Solid and Metallic
Gloss at 60º | ASTM D523 | Solid 90+ & Metallic 70+
VOCs | - | ≤ 3.6 lbs./gal. (≤ 431 g/L), less exempts
Cure | - | Oven Time/Temp: 20-60 min @ 100-180°F Air Dry*: To Touch: 45 min To Handle: 2 hrs
Performance Properties* |  | 
Pencil Hardness | ASTM D3363 | 2H
Conical Mandrel Bend | ASTM D522 | 1/8”
Adhesion | ASTM D3359 | 5B
Humidity Resistance | ASTM D2247 | 1000 hours
Weatherometer | SAE J2527 ASTM G155-05A | 1000 hours
Compatible Products
Primers: Liquid - Spectracron SEP78278, SEP78284, SEP80613 E-Coat – POWERCRON® P6000CX
*results obtained over iron phosphate pretreatment with electrocoat primer on CRS panels.
Key Features
Metallic color palette
Wide application window
Onsite mix line capable
Class A appearance
Spectracron® HST
Solventborne Topcoat
*Requires accelerator. Excess film thickness will retard dry times. Do not apply at temperatures below 50°F(10°C). For specific product VOC information refer to the environmental data sheet (EDS).

## Slide 3: Spectracron® HST
Solventborne Topcoat
Truck Bodies
Refuse Trucks
Recreation Vehicles
Additional end-use photos

## Slide 4: Spectracron® HST
Specifications and Approvals
McNeilus
Solventborne Topcoat