## Slide 1: Spectracron® SEP
Solventborne Primer – SEP79745
Availability | Technology | Coating Type | Chemistry | Substrates
USCA – Stock | Liquid Solventborne | Primer | 2K Zinc Rich Epoxy | Blasted Steel
PPG Segments
Transportation
Suggested Uses
Truck Chassis
Truck Trailers
Features | Potential Customer Benefits
Outstanding corrosion performance | Provides high level of protection for assets and increases product longevity
Ambient cure capable | Reduces energy consumption and process costs
Wide recoat window | Provides flexibility in process conditions
Wet-on-wet capable | Increases throughput and decreases process cost
≤3.0 VOCs and specifically formulated without HAPs | Reduces cost related to environmental controls
Initially introduced into the transportation segment this primer technology has demonstrated value to our customers.

## Slide 2: Spectracron® SEP
Solventborne Primer – SEP79745
Product Characteristics* |  | 
Color | - | Gray green
Gloss at 60º | ASTM D523 | 30-60
VOCs | - | ≤ 3.0 lbs./gal. (≤ 359 g/L), less exempts
Cure | - | Oven Time/Temp: 20-30 min @ 140-160°F Air Dry*: To Touch: 30 min To Handle: 50-90 min
Wet on Wet | - | Flash time: >30min
Recoat window | - | 7 days
Performance Properties* |  | 
Adhesion | ASTM D3359 | 5B
Pencil Hardness | ASTM D3363 | 2H
Impact Resistance, Direct | ASTM D2794 | > 60 in-lbs
Humidity Resistance | ASTM D2247 | >1,000 hours
Salt Spray Resistance | ASTM B117 | ≥2,000 hours
Cyclic Corrosion | SAE J2334 | ≥60 cycles
Compatible Products
Topcoats: Spectracron HSI and HSU
*results obtained over blasted steel. Performance dependent on pretreatment used.
Key Features
Outstanding corrosion performance
Ambient cure capable
Wide recoat window
Wet-on-wet capable
*Excess film thickness will retard dry times. Do not apply at temperatures below 50°F(10°C). For specific product VOC information refer to the environmental data sheet (EDS).