## Slide 1: Spectracron® SEP
Solventborne Primer – SEP76001, SEP83052 & SEP81601
Availability | Technology | Coating Type | Chemistry | Substrates
USCA – MTO | Liquid Solventborne | Primer | 2K Epoxy | Blasted Steel, Cold Rolled Steel, Hot Rolled Steel, Galvaneal Steel
PPG Segments
Agriculture and Construction Equipment
General Industrial
Transportation
Suggested Uses
Agriculture Equipment
Concrete Mixers
Construction Equipment
Generators
Refuse Trucks
Truck Bodies and Beds
Structural Steel
Features | Potential Customer Benefits
Strong corrosion performance | Protects assets and increases product longevity
Common catalyst with topcoat | Reduces inventory cost and complexity
Wet-on-wet capable | Increases throughput and decreases process cost
Customizable colors | Allows differentiation through color
Fast drying | Lowers cost and increases throughput
Ready to sand in less time | Increases throughput
Initially introduced into the OEM agriculture and construction equipment segment this primer technology has demonstrated value to our customers.

## Slide 2: Spectracron® SEP
Solventborne Primer – SEP76001, SEP83052 & SEP81601
Product Characteristics* |  | 
Color | - | Gray, Buff, Black, tintable
Gloss at 60º | ASTM D523 | ≤ 80
VOCs | - | ≤ 3.2 lbs./gal. (≤ 383 g/L), less exempts
Cure | - | Oven Time/Temp: 30-60 min @ 140-180°F Air Dry*: To Touch: 20 min To Handle: 60 min
Wet on Wet |  | Flash time: 5 – 20 min
Sandable |  | With accelerator: 45-60min
Performance Properties* |  | 
Adhesion | ASTM D3359 | 5B
Pencil Hardness | ASTM D3363 | 4H
Conical Mandrel Bend | ASTM D522 | 1/8”
Impact Resistance, Direct / Reverse | ASTM D2794 | 60 / 40 in-lbs
Humidity Resistance | ASTM D2247 | 1,000 hours
Salt Spray Resistance | ASTM B117 | 1,000 hours
Compatible Products
Topcoats: Spectracron HSL, HSI, HSU and VRPT
*results obtained over iron phosphate pretreated CRS panels. Salt spray performance dependent on pretreatment used.
Key Features
Strong corrosion performance
Common catalyst with topcoat
Wet-on-wet capable
Customizable colors
*Requires accelerator. Excess film thickness will retard dry times. Do not apply at temperatures below 50°F(10°C). For specific product VOC information refer to the environmental data sheet (EDS).

## Slide 3: Spectracron® SEP
Solventborne Primer – SEP76001, SEP83052 & SEP81601
Generators
Agriculture equipment
Refuse Trucks
Additional end-use photos