## Slide 1: Envirocron® High Transfer Efficiency
Polyester powder coatings with high-transfer efficiency (HTE) properties
Availability | Technology | Coating Type | Chemistry | Substrates
USCA | Powder | Topcoat | Polyester TGIC Polyester HAA | Cold-rolled steel, hot-rolled steel, aluminum, iron
PPG Segments
Building Products-Extrusions
General Industrial
Agriculture and Construction Equipment
Transportation
Wheels
Suggested Uses
Complex parts/patterns
Wired goods: baskets
Shopping carts
Metal shelving
Patio furniture
Features | Potential Customer Benefits
Up to 85% first-pass transfer rates | Reduces labor, material and utilities costs
Improved wrapping on complex parts and shapes | Decreases parts rejects and needs to touch-up
Improved powder film thickness control | Reduces powder use while achieving same quality
Lower cure option (320°F) | Reduces energy use due to lower oven set point
Ample gloss range (@60, 15 to 95) | Meets various customers specifications for finish product
Durable and Ultradurable formulations | Colors last longer
*Refer to powder cure curves for details

## Slide 2: Envirocron® High Transfer Efficiency
Waste saving first-pass transfer efficiency
Energy saving 10 min cure at 350°F
Key Features
Reduced coating film thickness while maintaining quality
Formulated for complex parts and shapes
Product Characteristics | Envirocron HTE 03 | Envirocron HTE 04 | Envirocron HTE Durable | Envirocron HTE Ultra-Durable
Specifications | AAMA 2603 | AAMA 2604 |  | 
Color | Full range | Full range | Full range | Full range
Gloss @ 60˚ (ASTM D523) | 15-95* | 15-95* | 15-95* | 15-95*
Substrate | Aluminum | Aluminum | Cold-rolled steel, hot-rolled steel, aluminum, iron | Cold-rolled steel, hot-rolled steel, aluminum, iron
* Lower gloss can be achieved for textured finishes |  |  |  | 
Performance Properties |  |  |  | 
Hardness (ASTM D3363) | 2H minimum | 2H minimum | 2H minimum | 2H minimum
Adhesion (ASTM D3359) | 5B | 5B | 5B | 5B
Salt Spray Resistance (ASTM B117) | 1,500 hours | 3,000 hours | Al: 1500 hrs Steel: 1000 hrs | Al: 3000 hrs Steel: 1000 hrs
Humidity Resistance (ASTM D2247) | 1,500 hours | 3,000 hours | Al: 1500 hrs Steel: 1000 hrs | Al: 3000 hrs Steel: 1000 hrs
Chalking Resistance (ASTM D4214) | Up to 2 years | 5 years |  | 
South Florida Exterior Exposure | Up to 2 years | 5 years |  | 
Specifications
Envirocron ‘03 meets AAMA 2603
Envirocron ‘04 meets AAMA 2604
Notes: AAMA 2604, 2003

## Slide 3: Envirocron® High Transfer Efficiency

## Slide 4: Internal Only
Selected colors with gloss range
Lower gloss can be achieved for textured finishes. † Product gloss range is specified with a 60˚ angle measurement value
The color chips in this selector cannot be considered totally accurate color matches, and are not to be used as approved standards. The technical data presented in this document is based upon information believed by PPG to be currently accurate. However, no guarantees of accuracy, comprehensiveness or performance are given or implied. Continuous improvements in coatings technology may cause future technical data to vary from what is in this document. Contact your PPG representative for the most up-to-date information.